| Typical Physical Properties |
| --- |
| Hardness, ASTM D-2240 | Shore A | 88 |
| Hardness, ASTM D-2240 | Shore D | 42 |
| Elongation, 25° C, ASTM D-412 | % | 320 |
| Tensile Strength 25° C, ASTM D-412 | PSI | 3000 |
| Tear Strength, ASTM D-624 | PLI | 295 |
| Taber Abrasion, C-17 / 1000 cycles | mg loss | 95 |
| Water Absorption, 25° C / 30 days | % | 3 |
| Theoretical coverage @ 62.5 mils (1.6 mm) | 25 ft²/gal |
| Theoretical coverage @ 125 mils (3.2 mm) | 13 ft²/gal |
| Application Requirements |
| Application Method | high pressure machine |
| Minimum Temperature | °F | 145 |
| Minimum Working Pressure | PSI | 1750 |
| Minimum Mix Time | min | 30 |
| Recoat Window | hours | 2 |
| Processing Characteristics |
| Solids by Weight and Volume | % | 100 |
| Mix Ratio by Volume | 1:1 |
| Gel-Free Time | sec | 10-14 |
| Tack-Free Time | sec | 18 |
| Typical Properties Component A (ISO) |
| Viscosity @ 25° C | mPa·s | 350 - 650 |
| Specific Gravity @ 25 ° C | 1.12 |
| Weight @ 25 ° C | lbs/gal | 9.58 |
| Appearance @ 25°C: | liquid |
| Typical Properties Component B (Resin) |
| Viscosity @ 25° C | mPa·s | 200 - 400 |
| Specific Gravity @ 25°C: | 1.01 |
| Weight @ 25 ° C | lbs/gal | 8.50 |
| Appearance @ 25°C: | liquid |

Product Description:

Silver 65 is a premier Bedliner product with excellent physical properties and shine.

Ideal for:

- OEM “Factory” Appearance

- High Polyurea Content

- Excellent strength and elongation

- High shine

Applications:

Silver 65 is a spray on high polyurea content coating designed for Bedliner applications, general waterproofing, abrasion and chemical resistance. Great for new and experienced sprayers, this product is high in strength and elongation, and is forgiving in high moisture and humidity areas.

Storage and Handling:

Containers for both isocyanate and resin (components A and B) components need to be tightly closed to prevent moisture contamination. Make sure to change your dessicant filters and drum rings to ensure no air is able to seep into the ISO drums. Do not reseal if contamination is suspected. Storage for both components should be maintained between 59 (F (15 (C) and 77 °F (25 °C). For best results, this product should not be allowed to freeze, although it may be re-heated in a well ventilated oven for a period of time to re-liquefy solid particles. To avoid product degradation, product temperature during re-heating should not exceed 140°F (60°C). Exposure to temperatures over 400°F (204°C) can create excessive pressure potentially causing containers to rupture.  Shelf life is 6 months for isocyanate component and 12 months for resin component as long as the product is not exposed to air or moisture.

Health and Safety Information:

Refer to this product’s Material Safety Data Sheet (MSDS) which provides information concerning the health and safety precautions that must be observed when handling any of the products listed above.  Before working with these products, it is the user’s responsibility to read and become familiar with the available information on its hazards, proper use and handling.